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	Clean pakaging 
Water resistant
Vacuum bag -quality warranty
Extended shelf life
Resistant to mechanical shocks

100% recyclable
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Product description
Rimano® GLET is a fine, white gypsum plaster for interior finishes, easy to sand. 

Intended use
· It is used for interior finishing, applied on previously levelled substrates: undercoats based on gypsum, thick smoothing plasters based on gypsum. It can be applied in one or several thin layers of up to 2 mm thickness.

· It can also be used in renovation purposes and repairing of damaged interior plastering.

The substrate
· The substrate must be clean, dust-free, oil-free, tars-free, soot-free, unfrozen, dry and protected from excessive moisture.
· Highly absorbent areas (e.g. very dry undercoat) must be sprinkled / wetted thoroughly with clean water or treated with Rikombi Grund to equalize absorption.
· Areas with low adhesion must be treated with Rimano® Grund to ensure adhesion.
· Do not apply the product on surfaces made of wood, plastic.
· In case of previously painted surfaces (washable paints, oil based paints, enamels, alkyd paints, etc.). it is recommended to remove the whole layer of paint / other material and treat the surface with Rimano® Grund to ensure adhesion.
Application conditions
· The temperature of air, material and substrate must be above +5°C and below 35°C. 

· Under excessive heat, ventilation or cold, with plastering work in progress or freshly finished plastering, must be adequately protected to normalize temperature and reduce the intensity of air currents.
· In closed areas appropriate ventilation, without intense air currents, must be provided, in order to ensure proper product drying.

Application
Material preparation

· Sprinkle the product in clean water (never vice versa!): approx. 20 kg of powder in approx. 18 litres of water.

· Wait for about 3 minutes for the entire quantity of powder to be soaked in the water, then stir with a mixer until a homogeneous paste is obtained. 
· Attention! Excessive mixing causes shorter working time.
· After mixing no more powder can be added to the resulting paste (lumps will form!). It is possible to add water in the paste to obtain a thinner consistency.

· A second paste mixing is not required.

· Do not mix Rimano® GLET with other materials.
· In the case of non-compliance with the Product Technical Data Sheet quality defects may occur in the preparation, application and finishing of the product.
Method of application
· The application must be manual in a single layer or in successive layers, wet on wet or wet on dry until smooth and flat white surfaces have been obtained.

· For a perfect finishing which does not require sanding, the plastered surface may be smoothed with the trowel after slight wetting with a moist brush. 

· If needed, the surface may be easily sanded after being completely dried.
· The final surface, resulted after the product is completely dried and hardened, is a perfect background for applying the final finishing coat (ex. paint or wallpaper).
Tools required 
· Clean tools must be used (trowel and spatula, hawk, etc.). 

· Attention! Powder remains or hardened plaster remains on tools or work containers, as well as other impurities may shorten the product working time.

· The tools must be cleaned using clean water immediately after use.

Product storage and handling

· The product must be kept in a dry place, in the original sealed bag and protected from bad weather.
· In case of partial use, the bag must be closed as well as possible (to avoid the transfer of moisture from the air). It is recommended to be used as soon as possible.
· The product shelf life is printed on the bag.
Occupational and environmental protection measures
· It is recommended to work with appropriate protective equipment: protective clothing, safety glasses, gloves and dust mask. 

· Avoid contact with the eyes (if necessary rinse with plenty of water and seek medical advice), prolonged contact with the skin, ingestion/ inhalation of the product.
· It is recommended to open carefully the bag and manipulate the powder with care in order to avoid dusting.
· The waste resulted from the packaging and product use will be treated according to legal provisions in force. 
· Vacuum packaging 100% recyclable.
· Read and follow the recommendations in the Product Safety Data Sheet.

Techical data
The product parameters presented below refer to temperature requirements of 23±2°C and relative air humidity of 50±5%.
	Standard of reference
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 under 
SR EN 13279-1:2009

	Class
	B1/20/2

	Composition 
	white plaster, mineral compounds and additives

	Fire reaction class
	A1

	Finesse
	99% under 200μm

	Adhesion
	>0.1* N/mm2

	Flexural strength 
	>1* N/mm2

	Compressive strength 
	>2* N/mm2

	Working time
	approx. 70 min.

	Powder/water ratio
	20 kg of powder / 18 l of water

	Material consumption
	0.9 kg/m2/mm

	Packaging (bag)
	20 kg (polyethylene bag)

	Pallet 
	54 bags


*Limit values indicated by the harmonized standard (SR EN 13279-1:2009).
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The information in this Product Technical Data Sheet is based on testing at Saint-Gobain laboratories. Indications on material preparation and application are correlated to each product. Deviations from these lead to lower expected product performance and reduce any associated obligations related to product warranties. The user shall abide by any potential protected commercial rights and legal provisions at the expense thereof. Any modifications to the product will be made in accordance with the legislation in force and within the reference standard.
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